## Slide 1
Juan Carlos Salcedo-Reyes, Ph.D.
SEMINARIO QHE
GaAs
Intrinsic Electron Concentration
Fermi Level
Energy Band Gap
Hole Effective Mass
Electron Effective Mass
Nc: Effective Density of States Function (4.35  1017 cm-3 @ 300 K)
Ev
EFi
Ec
Eg (1.424)
VL
e (4.07)
4.0
4.5
5.0
5.5
0.674


## Slide 2
Juan Carlos Salcedo-Reyes, Ph.D.
SEMINARIO QHE
AlxGa1-xAs
VL
EFi
Energy Band Gap
Eg (1.82)
Intrinsic Electron Concentration
(ni= 1.103103 cm-3 , @ x= 0.32)
(0.0896 me @ x = 0.32)
Electron Effective Mass
Hole Effective Mass
Fermi Level
GaAs
Ev
EFi
10
Ec
Eg (1.424)
Intrinsic Electron Concentration
Fermi Level
VL
Energy Band Gap
Hole Effective Mass
Electron Effective Mass
e (4.07)
Nc: Effective Density of States Function (4.35  1017 cm-3 @ 300 K)
4.0
4.5
5.0
5.5
0.674
e (3.38)
Ec
Ev
0.9414

Electronic affinity

## Slide 3
Juan Carlos Salcedo-Reyes, Ph.D.
SEMINARIO QHE
Amphoteric Impurities
Si
AlxGa1-xAs
Donor
Aceptor
Donor Ionization Energy
(Ed = -8.9 meV @ x= 0.32)
Distance donor electron – donor impurity ion
(rd = 25.77ax, @ x=0.32)
a0 : Bohr radius
VL
EFi
Eg (1.82)
Ev
EFi
Ec
Eg (1.424)
VL
e (4.07)
4.0
4.5
5.0
5.5
0.674
e (3.38)
Ec
Ev
0.9414

AlxGa1-xAs
GaAs
Dielectric constant
Ed

## Slide 4
Juan Carlos Salcedo-Reyes, Ph.D.
SEMINARIO QHE
GaAs

Total electron concentration (intrinsic + donors)
Si-AlxGa1-xAs
Nd = 11018 cm-3 (Na = 0)
ni = 1.103103 cm-3 (@ x=0.34)
n0= 1016 cm-3 (majority carrier electron concentration)
p0= 10-11 cm-3 (minority carrier hole concentration)
EF - EFi= 0.890 eV
Fermi level
VL
EFi
Eg (1.82)
Ev
EFi
Ec
Eg (1.424)
VL
e (4.07)
4.0
4.5
5.0
5.5
0.674
e (3.38)
Ec
Ev
0.9414

Ed
EF
51.4 meV

## Slide 5
Juan Carlos Salcedo-Reyes, Ph.D.
SEMINARIO QHE
Heterojunctions: Energy bandgap has a discontinuity at the junction interface. Lattice match in important (dislocations and surface states). Straddling gap (type I) heterostructures. Anisotype heterostructure (different dopand type). Electron affinity rule (Ec and Ev discontinuity exist in the heterojuntion interface)
GaAs
 (4.74)
Si-AlxGa1-xAs
VL
EFi
Eg (1.82)
Ev
EFi
Ec
Eg (1.424)
VL
e (4.07)
4.0
4.5
5.0
5.5
0.674
e (3.38)
Ec
Ev
0.9414

Ed
EF
51.4 meV
Ec=e(- )=0.69
Ev=0.294
 (4.32)
Eg=Ec-Ev=0.396
Ec
Ev

## Slide 6
Juan Carlos Salcedo-Reyes, Ph.D.
SEMINARIO QHE
Heterojunctions: Energy bandgap has a discontinuity at the junction interface. Lattice match in important (dislocations and surface states). Straddling gap (type I) heterostructures. Anisotype heterostructure (different dopand type). Electron affinity rule (Ec and Ev discontinuity exist in the heterojuntion interface)
GaAs
Si-AlxGa1-xAs
EFi
Eg (1.82)
Ev
EFi
Ec
Eg (1.424)
4.0
4.5
5.0
5.5
0.674
Ec
Ev
0.9414
Ed
EF
51.4 meV
Ec=e(- )=0.69
Ev=0.294
Eg=Ec-Ev=0.396
Ec
Ev

## Slide 7
Juan Carlos Salcedo-Reyes, Ph.D.
SEMINARIO QHE
Heterojunctions: Energy bandgap has a discontinuity at the junction interface. Lattice match in important (dislocations and surface states). Straddling gap (type I) heterostructures. Anisotype heterostructure (different dopand type). Electron affinity rule (Ec and Ev discontinuity exist in the heterojuntion interface)
GaAs
Si-AlxGa1-xAs
EFi
Ec
Ec=0.69
Ev=0.294
Eg=Ec-Ev=0.396
1.0
0.674
Ec
EF
51.4 meV
Ec(0.69)
0.5
0.75
0.25